## Slide 1: Composites

## Slide 2: What is a composite?
Can you think of any composites that you might use every day?
Notes: What is a composite? Can you think of any composites that you might use every day?
https://www.polleverywhere.com/free_text_polls/ZYuZRfIPrRuC8Sl

## Slide 3: What is a composite?
Notes: These examples include both natural and engineered composites that students may be familiar with from their everyday lives. Bone, wood and nacre (the seashell) are all natural composites that combine stiff and compliant materials to improve durability and maximize functionality.
The engineered composites include concrete (cement + gravel), polymer-based carbon-fiber composites (bicycle, plane and wind turbine) and metal matrix composites (the turbine and tank applications).

## Slide 4: Composites combine properties not found in a single material

## Slide 5: How do we define strength and toughness?
Strength: high resistance to deformation
Toughness: high resistance to fracture

## Slide 6: For example:
Notes: These Ashby plots compare the properties of strength vs. density (specific strength) on the left and strength vs. toughness on the right. Toughness defines a materials resistance to crack or fail while strength defines a materials resistance to deformation or change in shape.

## Slide 7: Why is the specific strength of ceramics so much higher?
Notes: Why is the specific strength of ceramics so much higher?
https://www.polleverywhere.com/free_text_polls/fIgKRcVkMZurehL

## Slide 8: Why is the specific strength of ceramics so much higher?
Notes: Answer: Bonding – strength of covalent or partially ionic bonds is much higher than most metallic bonds
and ceramics often combine (transition) metal with a much lighter element (like O, N or C)

## Slide 9: What are composites?
Matrix – light, protective
Reinforcement – strong, stiff
Composites generally have two parts:
  Polymers – most common
  Metal – ductile, conductive
  Ceramic – high temperature
  Carbon
  Glass
  SiC
  Natural fibers (hemp)

## Slide 10: Types of composites
Particle reinforced
Short fiber or whisker reinforced
Continuous fiber

## Slide 11: So what’s the actual combined property?

## Slide 12: Composite properties depend on fiber type and orientation
Young’s Modulus – E – measure of stiffness:
Notes: Applied force is distributed between the fibers and the matrix.
A good guess is that the force is distributed proportionally to the volume fraction of fibers. (Vf)

## Slide 13: A matrix material can transfer load from one fiber to another
Matrix can transfer load from one fiber to another
Interface is key!!
Notes: Talk about sizing fibers

## Slide 14: Fiber/matrix interfaces can deflect cracks and dissipate energy
Fiber/matrix interfaces can deflect cracks and dissipate energy

## Slide 15: Ex – energy dissipation
https://www.youtube.com/watch?v=JUhopbbHirA

## Slide 16: Where do composites fit?